RTCD298  SERIES　　　（ 105℃ 10000H）

- Compliant to the RoHS directive.

- 105℃ 10000H long life and high ripple current series.

■Specification

| Item | Performance Characteristics |
| --- | --- |
| Operating range | -25℃～+105℃ |
| Rated voltage range | 200V～450V |
| Capacitance tolerance | ±20% (20℃, 120Hz) |
| Leakage current | I≤0.01CV(μA) or1.5mA (Whichever is smaller) (20℃, after 5 minutes) C=Nominal capacitance(μF), V=Rated voltage(V) |
| Dissipation factor (20℃，120Hz) | UR(V) 200-400V 25 450V tanδ 0.15 0.45 0.20 |
| Stability at Low Temperature (Impedance ratio at120Hz) | UR(V) 200-400V 450V Z(-25℃)/Z(+20℃) 4 8 |
| Load Life | After applying rated voltage with specified ripple current for10000 hours at 105℃(the peak voltage shall not exceed the rated voltage), and then restored for 24 hours, capacitor shall meet the following requirement: Capacitance change Within ±20% of the initial value. Dissipation factor Not more than 250% of the initial specified value. Leakage current Not more than the initial specified value. |
| Shelf Life | After storing for 1000 hours at 105℃,UR to be applied for 30 minutes and then restored for 24 hours, capacitor shall meet the following requirement: Capacitance change Within ±20% of the initial value. Dissipation factor Not more than 200% of the initial specified value. Leakage current Not more than the initial specified value. |
| Standard | JIS C 5101-4 |

■Coefficient of rated ripple current

| 温度(℃) | 40 | 55 | 70 | 85 | 105 |  | 频率(Hz) UR(V) | 50(60) | 120 | 300 | 1K | ≥10K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 系数 | 2.7 | 2.5 | 2.1 | 1.7 | 1.0 |  | 160-250 | 0.81 | 1.00 | 1.17 | 1.2 | 1.50 |
|  |  |  |  |  |  |  | 350-450 | 0.77 | 1.00 | 1.16 | 1.41 | 1.43 |

■Drawing                                Unit：mm

*:Shorter terminal is: 4.0±0.5mm

■RTCD297 Dimensions

| Rated Voltage code (V.DC) | Capacitance ( μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 105℃, 120Hz (Arms) | Part number |
| --- | --- | --- | --- | --- | --- |
| 200 2D (250) | 560 | 30X30 | 0.15 | 1.50 | RTCD2982D561KR030M |
|  | 680 | 30X35 | 0.15 | 1.70 | RTCD2982D681KR035M |
|  | 820 | 30X40 | 0.15 | 2.00 | RTCD2982D821KR040M |
|  |  | 35X30 | 0.15 | 2.00 | RTCD2982D821KS030M |
|  | 1000 | 30X45 | 0.15 | 2.20 | RTCD2982D102KR045M |
|  |  | 35X35 | 0.15 | 2.20 | RTCD2982D102KS035M |
|  |  | 40X30 | 0.15 | 2.17 | RTCD2982D102KB030M |
|  | 1200 | 35X40 | 0.15 | 2.40 | RTCD2982D122KS040M |
|  |  | 40X35 | 0.15 | 2.45 | RTCD2982D122KB035M |
|  | 1500 | 35X50 | 0.15 | 2.81 | RTCD2982D152KS050M |
|  |  | 40X40 | 0.15 | 2.79 | RTCD2982D152KB040M |
|  | 1800 | 40X50 | 0.15 | 3.24 | RTCD2982D182KB050M |
| 250 2E (300) | 390 | 30X30 | 0.15 | 1.30 | RTCD2982E391KR030M |
|  | 470 | 30X35 | 0.15 | 1.42 | RTCD2982E471KR035M |
|  | 560 | 35X30 | 0.15 | 1.58 | RTCD2982E561KS030M |
|  | 680 | 30X45 | 0.15 | 1.80 | RTCD2982E681KR045M |
|  |  | 35X35 | 0.15 | 1.76 | RTCD2982E681KS035M |
|  | 820 | 30X50 | 0.15 | 2.03 | RTCD2982E821KR050M |
|  |  | 35X40 | 0.15 | 2.01 | RTCD2982E821KS040M |
|  |  | 40X30 | 0.15 | 1.96 | RTCD2982E821KB030M |
|  | 1000 | 35X45 | 0.15 | 2.30 | RTCD2982E102KS045M |
|  |  | 40X35 | 0.15 | 2.27 | RTCD2982E102KB035M |
|  | 1200 | 35X50 | 0.15 | 2.55 | RTCD2982E122KS050M |
|  |  | 40X40 | 0.15 | 2.53 | RTCD2982E122KB040M |
|  | 1500 | 40X50 | 0.15 | 2.96 | RTCD2982E152KB050M |
|  | 1800 | 40X60 | 0.15 | 3.39 | RTCD2982E182KB060M |
| 400 2G (450) | 220 | 30X35 | 0.15 | 1.00 | RTCD2982G221KR035M |
|  | 270 | 30X40 | 0.15 | 1.15 | RTCD2982G271KR040M |
|  |  | 35X30 | 0.15 | 1.13 | RTCD2982G271KS030M |
|  | 330 | 30X45 | 0.15 | 1.29 | RTCD2982G331KR045M |
|  |  | 35X35 | 0.15 | 1.26 | RTCD2982G331KS035M |
|  |  | 40X30 | 0.15 | 1.28 | RTCD2982G331KB030M |
|  | 390 | 30X50 | 0.15 | 1.44 | RTCD2982G391KR050M |
|  |  | 35X40 | 0.15 | 1.43 | RTCD2982G391KS040M |
|  | 470 | 35X45 | 0.15 | 1.60 | RTCD2982G471KS045M |
|  |  | 40X35 | 0.15 | 1.58 | RTCD2982G471KB035M |
|  | 560 | 35X50 | 0.15 | 1.79 | RTCD2982G561KS050M |
|  |  | 40X40 | 0.15 | 1.78 | RTCD2982G561KB040M |
|  | 680 | 40X50 | 0.15 | 2.05 | RTCD2982G681KB050M |
|  | 820 | 40X60 | 0.15 | 2.36 | RTCD2982G821KB060M |
| 450 2W (500) | 220 | 30X40 | 0.20 | 1.04 | RTCD2982W221KR040M |
|  |  | 35X30 | 0.20 | 1.02 | RTCD2982W221KS030M |
|  | 270 | 30X45 | 0.20 | 1.19 | RTCD2982W271KR045M |
|  |  | 35X35 | 0.20 | 1.16 | RTCD2982W271KS035M |
|  | 330 | 30X50 | 0.20 | 1.33 | RTCD2982W331KR050M |
|  |  | 35X40 | 0.20 | 1.32 | RTCD2982W331KS040M |
|  | 390 | 35X45 | 0.20 | 1.48 | RTCD2982W391KS045M |
|  | 470 | 35X50 | 0.20 | 1.64 | RTCD2982W471KS050M |
|  | 560 | 40X60 | 0.20 | 1.98 | RTCD2982W561KB060M |